## Slide 1
E-mail: denchev@dep.uminho.pt
Nanostructure Development in Multicomponent Polymer Systems and Its Characterization by Synchrotron X-ray Scattering
Synchrotron Radiation in Polymer Science
Madrid, 2015
Z. Denchev, N. Dencheva
Institute for Polymers and Composites/I3N Associated Laboratory, University of Minho, Portugal
A. Stribeck
Institute of Technical and Macromolecular Chemistry, University of Hamburg, Germany
S. Roth
Photon Science at DESY, Hamburg, Germany

## Slide 2
Motivation and Goals
In-situ Microfibrilar Composites
Preparation and morphology
Static transcrystallinity characterization by WAXS
Fine crystalline stcruture by SAXS under strain
Polyamide 6 Micorcapsules containing Solid Materials
Preparation and morphology
Crystalline strcuture via microfocus WAXS
Conclusions
Outline
2

## Slide 3
Microfibrilar Composites - Preparation
3
Polymer 1 = PA6 (may contain up to 7.5% MMT, Cloisite® or Nanomer®)
= PA12
Polymer 2 = HDPE
Compatibilizer = YP (HDPE-MAH)
Fibrilation
TCL formation

## Slide 4
MFC Preparation
4
l
2
= 6.3
Extruder
Haul
-
off 1
Haul
-
off 2
Winder
Oriented
cable
Heating
Bath 2
Cooling
Bath 1
l
1
= 2.6
 | wt-% |  | wt-% Clay in PA6 |  | Pre-blended with extra PA6
HDPE | PA6 | YP | Nanomer | Cloisite | 
80 | 20 |  | 1.0 - 7.5 |  | yes
77.5 | 20 | 5 | 1.0 - 7.5 |  | yes
80 | 20 |  |  | 1 - 5 | yes
80 | 20 |  |  | 1 - 5 | no
77.5 | 20 | 5 |  | 1 - 5 | yes
77.5 | 20 | 5 |  | 1 - 5 | no
HDPE | PA6 | PA12 | YP
65 |  | 30 | 5
70 |  | 20 | 10
75 |  | 20 | 5
77.5 |  | 20 | 2.5
80 |  | 20 | 0
65 | 30 |  | 5
70 | 20 |  | 10
75 | 20 |  | 5
77.5 | 20 |  | 2.5
80 | 20 |  | 0

## Slide 5
MFC – Mechanical Properties
5
0
10
20
30
40
50
60
600
800
0
10
20
30
40
50
60
70
HDPE
6
5
4
3
2
1
Stress, MPa
Strain, %
1-
90/10/0
2-
80/20/0
3-
70/20/10
4-
75/20/5
5-
77.5/20/2.5
6-
65/30/5
TENSILE PROPERTIES HDPE/PA12/YP
TENSILE PROPERTIES HDPE/PA6/YP
0
20
40
60
80
100
600
800
0
10
20
30
40
50
60
70
5
4
6
3
2
1
HDPE matrix
Stress, MPa
Strain, %
1 - 90/10/0
2 - 80/20/0
3 - 70/20/10
4 - 75/20/5
5 - 7.5/20/2.5
6 - 65/30/5
TENSILE PROPERTIES HDPE/PA6/YP/MMT

## Slide 6
MFC – Morphology by SEM
6
20 μm
5 μm
UDP MFC 80/20/0
UDP MFC 80/20/0 + 5 % MMT
Fibril Ǿ = 500-800 nm
Fibril Ǿ = 1500-1800 nm
Fibril Ǿ = 100-400 nm
500 nm
OP 80/20/0

## Slide 7
MFC – synchrotron WAXS (DORIS, A2-beamlne)
7
(110) HDPE
(200) HDPE
(200) a PA6
80/20/0
70/20/10
PA6, %
HDPE, %
80/20/0
70/20/10
PA6/HDPE
55.7
50.8
44.3
49.2
1.032
1.257
HDPE/PA6/YP
1D WAXS
Oriented scattering
-
-
=
=
Oriented scattering
Isotropic scattering
Initial pattern
POLAR -- Stonybrook Technology and Applied Research Inc.
HDPE/PA6/YP
1D WAXS –peak fitting

## Slide 8
MFC – synchrotron WAXS
8
2D WAXS oriented
80/20/0
70/20/10
(110) HDPE
(200) HDPE
(020) g PA12
(040) g PA12
Isotropic scattering
f = PA12/HDPE
PA12, %
HDPE, %
90/10/0
70/20/10
65.3
73.8
34.7
26.2
HDPE/PA12/YP
1D WAXS
Oriented scattering
80/20/0
77.5/20/2.5
65/30/5
75/20/5
66.0
67.4
68.9
71.1
34.0
32.6
31.1
28.9
2.817
1.911
f
1.941
2.067
2.215
2.460
Oriented scattering

## Slide 9
Outline
2
1. MMT is present in both oriented and
isotropic scattering;
2. The isotropic part does not contain PA6.
HDPE/PA6/YP/MMT | PA6, % | HDPE, % | f
80/20/0/4 NM | 37.6 | 37.3 | 1.00
80/20/0/4 CL | 30.8 | 35.3 | 0.87
80/20/0/5 NM | 33.8 | 32.1 | 1.05
80/20/0/5 CL | 31.7 | 39.0 | 0.81
80/20/0/7.5 NM | 32.6 | 27.9 | 1.17
77.5/20/2.5/ 5 NM | 32.3 | 29.0 | 1.11

## Slide 10
MFC – Comparative Structure Studies by WAXS
10
10
2R2
2R1
L
TCL = R2 – R1
2R1 = ?
PA6, %
HDPE, %
80/20/0
70/20/10
f
55.7
50.8
44.3
49.2
1.03 : 1
1.26: 1
HDPE/PA6/YP
PA12, %
HDPE, %
90/10/0
70/20/10
65.3
73.8
34.7
26.2
HDPE/PA12/YP
80/20/0
77.5/20/2.5
65/30/5
75/20/5
66.0
67.4
68.9
71.1
34.0
32.6
31.1
28.9
2.817
1.911
f
1.941
2.067
2.215
2.460
Components of the WAXS
oriented scattering
HDPE/PA6/YP/MMT | PA6, % | HDPE, % | f
80/20/0/4 NM | 37.6 | 37.3 | 1.00
80/20/0/4 CL | 30.8 | 35.3 | 0.87
80/20/0/5 NM | 33.8 | 32.1 | 1.05
80/20/0/5 CL | 31.7 | 39.0 | 0.81
80/20/0/7.5 NM | 32.6 | 27.9 | 1.17
77.5/20/2.5/ 5 NM | 32.3 | 29.0 | 1.11
Macromolecules 43:4715 (2010)

## Slide 11
MFC – Comparative Structure Studies by WAXS
11
11
UDP MFC 80/20/0
UDP MFC 70/20/10
2R2 = 750 nm
2R2 = 500 nm
TCL = 100 nm
2R1 = 550 nm
2R1 = 350
TCL = 75 nm
HDPE/PA6/YP, no MMT
UDP MFC 80/20/0
UDP MFC 70/20/10
2R2 = 625 nm
2R2 = 560 nm
TCL = 43 nm
2R1 = 539 nm
2R1 = 457 nm
TCL = 52 nm
HDPE/PA12/YP, no MMT
HDPE/PA6/YP, with MMT
TCL = 156 nm
2R1 = 738 nm
UDP MFC 80/20/0/ 5% NM
2R2 = 1050 nm
TCL = 228 nm
2R1 = 864 nm
UDP MFC 80/20/0/ 5% CL
2R2 = 1320 nm
TCL = 245 nm
2R1 = 1260 nm
UDP MFC 80/20/0/ 7.5% NM
2R2 = 1750 nm
TCL = 173 nm
2R1 = 854 nm
UDP MFC 77.5/20/2.5 7.5 NM
2R2 = 1200 nm

## Slide 12
MFC – TEM and WAXS data comparison
12
UDP MFC 80/20/0
2R2 = 750 nm
2R1 = 550 nm
2R1 = 550 nm
HDPE/PA6/YP, no MMT
(model)
ca. 520 nm
ca. 90 nm
HDPE/PA6/YP, no MMT
(TEM image)
TCL = 100 nm

## Slide 13
SAXS with 2D Detection – Outputs
13
Raw SAXS curve
0.00
0.05
0.10
0.15
0.20
0
500
1000
Intensity, a.u.
s, nm
-1
0
50
100
150
200
250
300
g
/Q
Distance
1D Correlation Function
Interface Distribution Function
0
50
100
150
200
250
300
g/Q
Distance, angstr.
Oriented
Isotropic
3D Chord Distribution Function
Stribeck, 2001
+CDF
-CDF

## Slide 14
2D SAXS Data Treatment - CDF
14
Raw SAXS image
1. Background correction;
2. Calibration; 3. Reconstruction
4. Calculation of the positive and negative parts of the CDF
Real Space
+
-
pv Wave® – 4GL Programming Environment
Reciprocal Space

## Slide 15
MFC Precursors Structure – HDPE/PA6
15
PE/PA6/YP=80/20/0
PE/PA6/YP=70/20/10
Cyclic strain in HDPE/PA6 MFC
PA6
HDPE

## Slide 16
MFC Precursors Structure – HDPE/PA12
16
PE/PA12/YP=80/20/0
PE/PA12/YP=70/20/10
Cyclic strain in HDPE/PA12 MMT
PA12
HDPE

## Slide 17
MFC Precursors Structure – HDPE/PA6-MMT
17
PE/PA6/0 =80/20/0 +7.5% MMT
With nanoclay
+ Nanomer
+ Nanomer, + YP
+ Cloisite
+ Cloisite, + YP
Failure mechanisms with nanoclay

## Slide 18
MFC Structure – HDPE/PA6
18
+ CDF
- CDF
TCL (HDPE)
Fibril (PA6)
180ºC
MFC HDPE/PA6
30ºC

## Slide 19
MFC Structure – HDPE/PA6
19
MFC PE/PA6/YP = 70/20/10
MFC PE/PA6/YP = 80/20/0
Reversible strain-induced crystallization of matrix material

## Slide 20
Hybrid composite materials
with electro-conductive & magnetic properties
CM, IM
One-pot synthesis of PAMC
Viscous particles
Microcapsules
Multifaceted applications
Starting mixture
Monomer
Catalytic system
Payload
Solvent
Pay-loads used (1-10 wt.%):
Natural nanoclays, synthetic Al/Ti sillicates
Carbon allotropes – CB, CNT, CNF, GR, Fullerenes
Metal & Metal oxides – Cu, Al, Mg, Fe, Fe3O4
Smart multifunctional
particle
Functionalization & Conjugation
20

## Slide 21
Gradients of fillers by high-flux microfocus beam
22
P03 microfocus beamline

## Slide 22
Gradients in PAMC by microfocus – PA6/@MMT
23
Y1; X 1
Scanning along X
Y3; X 1-11
5/5μm

## Slide 23
Gradients in PAMC by microfocus – PA6/@MMT
24
Y10; X1-10
Y09; X1-10
Y08; X1-10
Y07; X1-10
Y11; X1-10
x01
x11
y11
y01
Scanning along Y

## Slide 24
25
Distribution of non-exfolliated MMT
Thickness distribution of the PAMC layer
PAMC@Nanomer 2 wt%
Non-homogeneous exfoliation of MMT
Gradients in PAMC by microfocus – PA6/@MMT

## Slide 25
Gradients in PAMC by microfocus – PA6/@MMT
26
Distribution of exfolliated MMT
Thickness distribution of the PAMC layer
PAMC@Cloisite 15A 2 wt%
Relatively homogeneous exfoliation of MMT

## Slide 26
27
Intensity of the Al reflection
Thickness of PA6 layer
PAMC@Al 5 wt%
PA6-covered metal platelets
Gradients in PAMC by microfocus – PA6/@Al 5%

## Slide 27
27
Intensity of the Fe3O4 reflection
PAMC@Fe3O4 5 wt%
PA6-covered metal platelets
Gradients in PAMC by microfocus – PA6/@Fe3O4 5%
Thickness of PA6 layer