## Slide 1
PolyChar 23
23rd World Forum on Advanced Materials Lincoln, Nebraska, U.S.A. May 11-15, 2015
e-mail: denchev@dep.uminho.pt
Structure Gradients by Microfocus Synchrotron X-ray Diffraction
in Shell-Core Polyamide Microcapsules
Zlatan Z. Denchev1, Nadya V. Dencheva1, Stephan Roth2
(1) I3N – Institute for Polymers and Composites, University of Minho, Department of Polymer Engineering, Guimarães, Portugal
(2) Photon Science at DESY, Notkestr. 85, Hamburg, Germany

## Slide 2
Objectives
Samples: PA6@ payloads microcapsules, synthesis by in-situ polymerization
Structure of polyamide materials by X-ray diffraction:
- Conventional WAXS
- Synchtrotron WAXS
- Microfocus high-flyx synchrotron WAXS
Conclusions
Outline:
2

## Slide 3
Hybrid composite materials
with electro-conductive & magnetic properties
CM, IM
One-pot synthesis of PAMC
Viscous particles
Microcapsules
Multifaceted applications
Starting mixture
Monomer
Catalytic system
Payload
Solvent
Pay-loads used (1-10 wt.%):
Natural nano-clays, Synthetic Al/Ti sillicates
Carbon allotropes – CB, CNT, CNF, Fullerenes
Metal & Metal oxides – Cu, Al, Mg, Fe, Fe3O4
Smart multifunctional
particle
Functionalization & Conjugation
PAMC
3

## Slide 4
Pay-loads used (1-10 wt.%):
Natural nano-clays (CLOISITE 15A, CLOISITE 20A );
Synthetic Al/Ti sillicates
Carbon allotropes – CB, CNT, CNF, Fullerenes
Metal & Metal oxides – Cu, Al, Mg, Fe, Fe3O4
One-pot synthesis of PAMC – reaction
Pat. Appl. 12345/2015
4

## Slide 5
Standard X-ray diffraction - PA6
5
Isotropic PA6
Predominantly  crystalline form
Oriented PA6
Predominantly  crystalline form

## Slide 6
Standard X-ray diffraction - loads
6
1 – (020) reflection of γ-PA6;
2 – (200); 2’ - (002/202) reflection of the α-PA6;
3 – (200) reflection of the γ-PA6;
4 – Opal CT reflection of NM;
5 – weaker reflections of the NM phase.
The inset shows the WAXS curve in the 0.1-1.0 nm-1 range of the scattering vector s.
2,
PA6 / 7.5 wt.% NM
‘
Pure nanoclays: NM @CL15A

## Slide 7
Standard X-ray diffraction
7
PA6/ 5 wt.% of Fe, Al….
1 – (200); 2’ - (002/202) reflection of the α-PA6;
2 – The strongest reflection of Fe3O4
Me

## Slide 8
Synchrotron X-ray diffraction
8
v
v
PA6 @ Cloisite 15ª, various %
Cloisite 15 A 2 wt%

## Slide 9
High-flux microfocus beam synchrotrons
9
P03 microfocus beamline

## Slide 10
Microfocus High-flux Synchrotron WAXS
10
Y1; X 1
Scanning along X
Y3; X 1-11
5/5μm

## Slide 11
Microfocus High-flux Synchrotron WAXS
11
Y10; X1-10
Y09; X1-10
Y08; X1-10
Y07; X1-10
Y11; X1-10
x01
x11
y11
y01
Scanning along Y

## Slide 12
12
Distribution of non-exfolliated MMT
Thickness distribution of the PAMC layer
PAMC@Nanomer 2 wt%
Non-homogeneous exfoliation of MMT
Microfocus High-flux Synchrotron WAXS

## Slide 13
Microfocus High-flux Synchrotron WAXS
13
Distribution of non-exfolliated MMT
Thickness distribution of the PAMC layer
PAMC@Cloisite 15A 2 wt%
Relatively homogeneous exfoliation of MMT

## Slide 14
14
PAMC@Cloisite20A 2 wt%
Homogeneous MMT distribution
Microfocus High-flux Synchrotron WAXS
Distribution of non-exfolliated MMT
Thickness distribution of the PAMC layer

## Slide 15
15
Intensity of the Al reflection
Thickness of PA6 layer
PAMC@Al 5 wt%
PA6-covered metal platelets
Microfocus High-flux Synchrotron WAXS

## Slide 16
16
Conclusions
High flux microfocus WAXS can determine microgradients in very fine layers of pulverulent composite materials;
3. Studying different scattering angle areas gives information about the filler size, distribution, matrix amount and polymorphism;
2. Relatively simple setups and data processing algorithms permit visualization of both layer thickness and load distribution in areas starting from 5x5 µ2;
4. Further development of the technique proposed will be the use of nanosized high-flux synchrotron beams.

## Slide 17
17
Acknowledgements
1. n-STEP – 07-0124-FEDER-00039 supported by the Programa Operacional Regional do Norte ON-2;
2. FEDER fund through the COMPETE-2020 Program and National Funds through FCT under the project UID/CTM/50025/2013;
3. DESY Photon Science Project No I-20130095 EC